74:02:04:53.01.  Bentonite grout requirements. Bentonite material manufactured for use as a drilling fluid does not meet the requirements for bentonite grout. For approval by the chief engineer, bentonite grout must contain a minimum of 20 percent solids by weight and have a minimum slurry density of 9.4 pounds per gallon and must be mixed according to the manufacturer's recommendations.

Source: 18 SDR 224, effective July 16, 1992.

General Authority: SDCL 46-2-5, 46-6-20, 46-6-27.

Law Implemented: SDCL 46-6-6.1, 46-6-10, 46-6-20, 46-6-27.